Solid Bar Compositions Containing Superior Abrasives

| Compound Grade | Abrasive Type | Binder Content | Product Colour | Hardness | Type of Metal | Type of Buff | Degree of Cut (metal removal) | Degree of Colour (brightness) |  | Description & Application |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| # TRIPOLI GRADES |  |  |  |  |  |  |  |  |  |  |  |
| # Tripomax E | Blended natural Tripoli | M | Brown | Medium | Non-ferrous | Ventilated cotton & stitched buffs including G.P. cottons | 7 |  | 7 |  | General purpose cut and polish for flatware |
| Tripomax Super | Special natural Tripoli | M | Light Brown | Medium | Non-ferrous | Ventilated cotton & stitched buffs including G.P. cottons | 8 |  | 9 |  | Very best Tripoli compound. Produces excellent finish & clarity. Fully saponifiable |
| # CUT-DOWN / BRUSHING GRADES |  |  |  |  |  |  |  |  |  |  |  |
| 2464 Abramax | Medium Fused Alumina | M | Grey | Hard / Firm | Ferrous | Treated & untreated sisal buffs | 8 |  | 5 |  | A cutting/brushing compound for first stage buffing process to remove 180/220 abrasive lines |
| # CUT AND COLOUR GRADES |  |  |  |  |  |  |  |  |  |  |  |
| Sunblue | Medium calcined alumina | L | Blue | Hard / Medium | All metal types | Stitched cotton or ventilated buffs or soft treated buffs | 6 |  | 8 |  | Finishing product for Stainless or cutting and colouring product for all other metal types |
| GlomaxYellow | Medium/fine calcined alumina | L | Yellow | Medium | All metal types. Plastics & veneers | Untreated sisal & sisal/cloth blended including ventilated & stitched cotton buffs | 8 |  | 7 |  | Medium cut & colour compound. Very clean in use, minimal residues, easy to clean |
| Maxfin | Special calcined alumina | L | Light green | Hard / Firm | All metal types | Untreated sisal buffs. Mill treated & untreated ventilated & stitched cotton buffs | 7 |  | 8 |  | Unique cut & colour compound for all round performance. To remove 360/400 abrasive lines |
| Nico Pink | Blended calcined alumina | M | Pink | Medium | All metal types | Graded cotton in full disc for stitched & unstitched buffs | 5 |  | 9 |  | Finishing bar with some cut. Greasier than Chromax Super |
| # Chromax Super | Very fine calcined alumina | L | White | Hard / Firm | All metal types | Graded cotton in full disc for stitched & unstitched buffs | 4 |  | 9 |  | Final white finishing compound provides fine lined finish with good reflectivity on all metals. Excellent preparation for Rouge bars |
| # Chromax Green | Very fine calcined alumina | L | Green | Firm | Ferrous | Cotton or sisal | 5 |  | 8 |  | Very good finishing product for all wheels, especially within the stainless and medical industry |
| Mirrormax | Calcined alumina | M | White | Medium | All metal types | Calico | 3 |  | 10 |  | Ultra fine finishing compound for use on soft cotton buff |
| # SPECIAL APPLICATION COMPOUNDS |  |  |  |  |  |  |  |  |  |  |  |
| Plastimax | Super fine calcined aluminas | L | Cream | Medium | Plastics & veneers | Soft, fine, ventilated & unstitched full disc buff | 2 |  | 8 |  | Super fine, soft abrasive compound for final finishing of plastics, polyester lacquers, acrylic & wood |
| Starmax SF | Ultra-fine iron oxide Rouge powder | L | Dark red | Medium | Brass, gold, silver, platinum | Very soft, fine, unstitched cotton & chamois leather buffs | 1 |  | 10 |  | Ultra-fine Rouge finishing compound, providing a scratch-free finish with high reflectivity. Some free grease. |

| Abrasive Types: |  | Types of Metal: |  |
| --- | --- | --- | --- |
| # Tripoli | A soft abrasive normally used on non-ferrous metals | Ferrous | Refers to steel or stainless steel or any metal containing iron |
| # Calcined Alumina | A hard abrasive, many different grades of hardness and particle sizes. Used on both ferrous and non-ferrous metals | Non-Ferrous | Refers to any metal which does not contain iron such as brass, aluminium and copper |
| # Fused Alumina | A very hard and tough abrasive, normally used on ferrous metals |  |  |
| Binder Content: |  | Type of Buff: |  |
| # H | High binder content necessary for heavy cutting operations (high metal removal). The binder is used to hold the abrasive particles onto the buff face | # Sisal | Used for high metal removal on ferrous metals |
| # M | Medium binder content is normal for compounds used for medium metal removal but results in good brightness | # Calico | Used for all applications except where very high metal removal is needed |
| # L | Low binder content for finishing compounds, giving high brightness and clean components |  |  |
| Hardness: |  | ## Cut & Colour Index – 1 = lowest 10 = highest |  |
| # Hard grades | Usually have lower binder contents and are used for finishing | 10 : 1 | Highest cut/lowest colour - rapid metal removal, semi-bright/lined finish |
| # Soft grades | Have high binder contents to help mop retention for cutting operations | 1 : 10 | Lowest cut/highest colour - minimal metal removal, fully bright/mirror finish |
|  |  | Note: The degrees of cut and colour are assessed on non-ferrous metal in the case of Tripoli formulations and on ferrous metals in the case of fused and calcined alumina. |  |